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TECHNICAL DATA

FOLIA ODBLASKOWA NEW FX
Soft Monomeric PVC with PET film

Color: white 
Surface: glossy

Specification
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Properties

PVC film thickness

PET film thickness

Glue thickness

Surface

Adhesive type

Release paper

Shelf life

Application temperature

Service life by specialist application

Under vertical outdoor exposure (normal climate of China)

Available Size



Test method

ISO 4591:1992

ISO 4591:1992
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Metric

75 micron Monomeric pvc film

93 micron PET film

25 micron glossy

Solvent polyacrylate,permanent adhesive,transparent

One side coated silicone paper, 110micron

Up to 2 years

Min.+10

Up to 1 year

1.24Mx45.7M

Ink printability
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Eco-solvent



Solvent

NOTE: All above information shall only used as a guide; buyers shall independently test and determine the products suitability. The mentioned data are average of test result and should not be used for the purpose of lawsuit or warranty

