Title: PosterColor X 180
Subject: High quality poster paper with blocking layer for advertising applicationsA bright white, barrier-coated, matt poster paper for indoor photographic and advertising applications. In combination with aqueous and latex inks, it guarantees a broad colour spec
Author: SIHL GmbH
Last saved by: Agnieszka Mikolas
Company: Atrium CP
Keywords: SIHL, 3257, PosterColor X 180

PLACARDS / POSTERS 

POSTERCOLOR	X	180 

matt 3257, 180 g/m^2

Wysokiej jakości papier plakatowy z warstwą blokującą do zastosowań reklamowych.

Biały, błyszczący, pokryty powłoką barierową, matowy papier plakatowy do zastosowań fotograficznych i reklamowych wewnątrz pomieszczeń. W połączeniu z atramentami wodnymi     i lateksowymi gwarantuje szerokie spektrum kolorów i wysoką gęstość optyczną. Powłoka barierowa zapewnia dobrą płaskość, nawet przy drukowaniu z dużą gęstością atramentu.

Cechy:

•	Doskonała reprodukcja kolorów
•	Wolny od rippinów , nawet przy drukowaniu dużymi ilościami tuszu 
•	Szybkie schnięcie
•	Wolny od kwasów

Wskazówki
W celu zachowania dobrej jakości materiału, należy go przechowywać i przetwarzać w warunkach względnej wilgotności 30-65% w temperaturze 10-30°C.

Dane techniczne:

Technologie

Właściwości

Nazwa | Wartość | Normy
Masa [g/m²] | 180 | ISO 536
Grubość [µm] | 190 | ISO 534
Białość CIE D65/2° | 155 | ISO 11476
Nieprzepuszczalność [%] | 98 | ISO 2471
Chromatyczność (D65/10°) | L*94.7 a*4.4 b* -15.2 | DIN 6174

08.01.2018	Page 1/1

The values stated above are only for orientation. Before using our print media please check its compatibility for your printer and the intended application. We cannot be held responsible for any mistakes resulting from technically modified printers and/ or inks. Product design changes to our products technical developments may be carried out without prior notice.